SUPPLIER CERTIFICATION			Today's Date: 2/8/2023

Supplier's Name and Address:                                      Purchaser’s Name and Address:
      Veratex, Inc.	                                                               Hexcel Composites Ltd, ‘M’ Stores
      534 W 42nd Street #8                                                    Duxford Cambridge
      New York, NY  10036  USA                                       CB2 4QD, United Kingdom
      Phone: 212 683 9300   Fax: 212 889 5573                   Phone: 01223838244  Fax: 01223838723

Date of Manufacture:   01/27/2023            Hexcel RMS and Issue:     8251 ISSUE  B
Material Description: Style V10401 100% Polyester Tricot Knit Fabric
Expiry Date:   2/8/2025      Batch Number:  20216/29260700    P.O. Number: 10PO0085606-2

Batch Number 20216/29260700  Specification:
•	Structure:		Tricot Knit
•	Chemistry:		PET (Polyester)
•	Fabric Width:	1308 mm
•	I.D. Cores:		7.62cm (3 Inches)
•	Weight:		30 gsm
•	Filaments:		20 Denier Monofilaments

Additional Requirements:

•	Each roll is to be individually packaged to prevent contamination before finishing
•	Maximum roll length 700 meters
•	All joints must be flagged with a minimum of 120 m between joints
•	The maximum pallet height shall be 1 meter

Packaging Requirements:

•	Packaging shall be adequate to prevent loss, damage or deterioration in transit and for up to one year of the product in storage
•	An advice note giving details of purchase order number, item description, item number, quantity and RMS number and issue shall accompany each delivery.
•	The advice note shall bear the individual piece  numbers and roll lengths.
•	Containers shall be marked with highly visible labels and marked as required for 3.3.2
_______________________________________________________________________________
Certificate of Conformity

This is to certify that the aforementioned fabric conforms with the PURCHASE REQUIREMENTS 

of _8251, Issue B.
	RMS

Signature:__________________________________  Date:__________________
	  	Claude Simon
______________________________________________________________________________________

Certificate of Analysis

This is to certify that the lot covered by this certification has been analyzed and conforms to the specifications set forth in section 3.1 of  RMS_8251, Issue B.

Signature:__________________________________ Dated:____________________
		Claude Simon