[image: image1.jpg]HEXCEL..



HEXCEL COMPOSITES
















RMS: 
8251, Issue C


       


   Duxford, Cambridge CB22 4QB, England.









Effective date: 












RAW MATERIAL SPECIFICATION






Page  1 of  2


[image: image1.jpg]1. RAW MATERIAL: CARRIER CARRIER V104/1 (V10401) PET 1305MM






1.1

DEFINITION & HEXCEL ITEM NUMBER(S)




1.1.1 V104/1 carrier is a Tricot knit PET fabric support used in adhesive film manufacture.




1.1.2 B710196


2. ORDERING REFERENCE: 
CARRIER V104/1 (V10401)PET 1305MM


2.1 
 APPROVED Suppliers:




2.1.1. Veratex, 160 Madison Avenue, New York, NY 10016, USA

2.2

APPROVED MANUFACTURING LOCATION:




2.2.1. As 2.1.1

2.3

LOT DEFINITION: Material of a single type, manufactured under the same conditions and processed at the same time.

3. PURCHASE REQUIREMENTS


3.1

TECHNICAL SPECIFICATION







PROPERTY




SPECIFICATION

3.1.1

Structure
 




Tricot Knit

3.1.2

Chemistry



   

PET (Polyester) 

3.1.3

Fabric width  




1305mm±15mm
3.1.4

I.D cores





7.62cm  (3 inches)

3.1.5

Weight 





30 gsm

3.1.6

Filaments





20 Denier monofilaments

3.2 ADDITIONAL REQUIREMENTS:




3.2.1
Each roll is to be individually packaged to prevent contamination before finishing.




3.2.2
Maximum roll length 700 metres.




3.2.3
All joins must be flagged, with a minimum of 120m between joins.

3.2.4
The maximum pallet height shall be 1 metre.

      3.3 
PACKAGING & LABELLING:

3.3.1
Packaging shall be adequate to prevent loss, damage or deterioration in transit and for up to one year of the product in storage. 

3.3.2 Each delivery shall be accompanied by an advice note giving details of :-

· Hexcel purchase order number, 

· Hexcel item number

· Item description

· Quantity 

3.3.3
The advice note shall bear the individual piece numbers & roll lengths.




3.3.4
Containers shall be marked with highly visible labels and marked as required for 3.3.2. 


3.4

SUPPLIER CERTIFICATION 




3.4.1 
Certification shall include the following details:





Suppliers name & address








Hexcel RMS & Issue




Material description





Date of manufacture









Expiry date







Batch number




Certificate of Analysis









Certificate of






Signature of certifying




quoting results conforming








Conformity







individual




to section 3.1


DOCUMENT APPROVAL
























APPROVAL STAMP

ELECTRONICALLY APPROVED
3.4.2
Certification shall accompany each delivery and should be addressed to ‘Hexcel Composites Goods 







Inwards Inspection’ at the address shown above.




3.4.3
Certificates & labels shall be written in the English language.

3.4.4
Hexcel reserve the right to periodically audit the suppliers facilities to assure conformance to the requirements of this 



RMS.




3.4.5
Material which does not meet the requirements of this specification is subject to rejection and may be returned to the 





supplier at the suppliers expense.

3.4.6
The Vendor shall supply a statement with each delivery certifying that the goods listed have been inspected and tested and conform to the full requirements of the purchase order and this RMS unless stated otherwise.  






This can be a separate document or part of the Certificate of Analysis or Advice note.  This statement of 






Conformance shall preferably be signed. 

Example statement of conformance:-






“Certified that unless otherwise stated above, the materials described heron have been manufactured, tested and 






Inspected in accordance with the terms of the applicable purchase order and conform to the specification quoted.”


3.5

SUPPLIER QUALITY CONTROL




3.5.1
The supplier shall maintain a recognised quality system.

3.5.2
The supplier shall ensure that there are no changes to the manufacturing location, product, process, raw materials, production line, test or control methods or designation without prior written agreement from Hexcel’s Quality 
Assurance department. The supplier shall notify Hexcel in writing at least twelve months in advance of any proposed change with a detailed work programme to demonstrate that the proposed change can be implemented without adverse effects on product quality



3.5.3
Traceability of a lot/batch to its test results & components must be maintained.




3.5.4
The supplier shall maintain records relating to quality and lot/batch history for a minimum of 10 years.


3.6
STORAGE & SHELF-LIFE REQUIREMENTS


The material shall comply with the specifications for (Supplier please advise)x months from the date of manufacture @ ambient temperature in clean dry conditions.


The material shall have at least y months of usable shelf-life remaining from the date of receipt at Hexcel.

(supplier tech sheet or internal agreement)
4. ON-RECEIPT INSPECTION


(for Hexcel Internal use only)


4.1 SAMPLING PLAN: Not Applicable


4.2
RELEASE REQUIREMENTS:






PROPERTY








SPECIFICATION





TEST METHOD

4.2.1
Compliance to this specification




RMS 8251, Issue C

4.4 SAFETY REQUIREMENTS:




4.4.1 
Refer to Hexcel Safety Data Sheet manual.

5.
SUPPLIER APPROVAL

	JOB TITLE
	NAME
	SIGNATURE
	DATE

	
	
	
	

	
	
	
	



CIRCULATION:


Supplier

Goods Inwards

 
(








(





(		








(








(








X








(








(








(











